## Slide 1: High-Fidelity Mesoscale Simulation of Melt-Pool Dynamics in Powder Bed Fusion using the KiSSAM Simulation Software for Additive Manufacturing
I. Valuev, S. Belousov, M. Bogdanova, A. Perepelkina, I. Iskandarova,
B. Korneev, A. Zakirov, B. Potapkin
Hipercone Ltd., Ezrat Israel st 14, Jerusalem, 9434314, Israel
∗ e-mail: belousov@hipercone.com, valuev@hipercone.com,
https://hipercone.com
https://kissam.cloud

## Slide 2: Contents
Motivation
KiSSAM multiphysics model
Materials and validation
Selected applications

## Slide 3: Motivation
Experiment?
Process parameter space is multidimensional
Process parameters adjustment is time-consuming…
Some things are hard to measure
High costs…
Why don’t we go for…
simulation?
Melt pool level simulation of the process:
melting
hydrodynamics
solidification
temperature history
Energy deposition
morphology:
roughness & porosity
microstructure, mechanical properties
Process outcome

## Slide 4: Replacing experiment with simulation
Accurate physically based numerical modeling of the entire technological cycle
Mesoscopic level of modeling – up to hydrodynamic physical effects in the melt pool
In-situ visualization of the modeling process
High performance / GPGPU support
Material quality characterization
KiSSAM

## Slide 5: High-fidelity simulation based on the multiphysics models capturing all the essential phenomena
Hydrodynamic solver based on thermal lattice Boltzmann method with volume of fluid free surface tracking
Phase transition solid / liquid
Surface tension and wetting
Marangoni convection
Drag force in mushy zone
Recoil pressure, mass and energy losses due to the strong evaporation from the liquid surface
Radiation cooling
Evaporated metal and chamber gas flow tracking
Multicomponent evaporation
Ray tracing with multiple reflections (for laser beam)
Sensors and detectors photodiode response simulation
Grain microstructure simulation at solidification same as CAFE model
Heat conduction in the bulk far from the melt-pool
Powder bed packing Discrete Element Method (DEM) solver with knife movement
Convection cooling
MC simulation of electron trajectories with elastic and inelastic scattering in metal (for electron beam)
(c)

## Slide 6: KiSSAM workflow
Unified input file
PowDEM solver
KiSSAM
solver
Output data
Post-processing scripts
Process parameters
Material parameters
Powder parameters
Scenario of experiment
Powder deposition
Layer generation with a knife movement
Hydrodynamics
Phase transition
Thermodynamics
Energy deposition
Energy loss
Geometry of a sample
Temperature history
Rendered images and cross sections of the meltpool
Absorbed energy
Optical sensors response
Back-scattered electron sensor response
Grain structure
Track parameters
Customized cross sections
Grain structure inverse pole figures
Process movie
Powder cleaner
Roughness and porosity analysis

## Slide 7: Simulation performance
KiSSAM is a high performance software implemented on CUDA C++ for NVIDIA GPUs.
Typical performance is faster than 0.5 hr per 1 ms of scanning time.
Performance scales with increasing performance of continually modernized GPUs
Simulation times are given for a single GeForce RTX 3090 24 GB GPGPU

## Slide 8: Physics-based material parameters
 Library of verified materials
Inconel 625
 Temperature dependent properties
Ti6Al4V
Al alloy AA5182
CoCr
Stainless steel SS316L
Thermal diffusivity
Heat capacity
Material absorbance
AlSi10Mg
NiTi
Surface tension
Snapshot from input.json

## Slide 9: Material properties validation workflow
Experimental data
Material properties
Simulation
In collaboration with

## Slide 10: Selected KiSSAM features and applications
Process map generation
Process optimization
Benchmark for simplified models
Full part high-fidelity mesoscale simulations
Grain structure simulation
Process monitoring
Surface quality and porosity simulation
Complex scanning strategies
Multi-beam PBF simulation

## Slide 11: Process maps: Identifying scanning beam parameters for producing smooth tracks
D. Nakapkin et.al. Finding Optimal Parameter Ranges for Laser Powder Bed Fusion with Predictive Modeling at Mesoscale, Sim-AM 2019 (2019)

## Slide 12: Process optimization: Influence of an increased layer thickness on the morphology of single tracks in AlSi10Mg Alloy
P = 350W, v = 0.9 m/s
M. Bogdanova et.al., Mesoscale Simulation of Laser Powder Bed Fusion with an Increased Layer Thickness for AlSi10Mg Alloy, J. Manuf. Mater. Process. 2024, 8, 7
Upper limits to the powder layer thickness at 160-190 um have been identified

## Slide 13: High-fidelity simulation as a benchmark for simplified models
J. Plewinski et.al., Impact of Modeling Assumptions on Simulated Melt Pool Dynamics Compared to High-Speed X-ray Observations, in: Mathematical Modeling of Weld Phonomena, vol. 14, p. 195 (2026)
KiSSAM simulation of a dynamic keyhole development overlaid over the X-ray synchrotron images of keyholing in stainless steel 1.4301.
Comparison of dynamical keyhole (KiSSAM) and
a fixed keyhole simulations (walBerla)
for assessing the flow in the meltpool
Melt pool characteristics and flow velocities obtained with KiSSAM are used to benchmark and tune the simplified model

## Slide 14: Simulating whole parts with mesoscale precision
Source | Beam width, um | Velocity, m/s | Power, W | Alloy
Laser | 100 | 0.99 – 1.529 | 241 – 300 | Inconel 625
The US Air Force Research Laboratory (AFRL) Additive Manufacturing (AM) Modeling Challenge Series
Schwalbach, E. J. et al. Integrating Materials and Manufacturing Innovation 10.3 (2021): 319-337
B.Korneev et al. A numerical study of powder wetting influence on the morphology of laser powder bed fusion manufactured thin walls Additive Manufacturing, V. 74, 103705 (2023)
Careful tuning of poorly known wetting properties allows accurate simulation of thin wall morphology

## Slide 15: KiSSAM as a digital twin: Optimizing part morphology with spot melting scanning strategy
Top: FF build, middle: BF build, bottom: SM build. Right: cross-section, left: longitudinal section through the middle of the wall (25 layers) is shown. Color represents layer number. Substrate is dark grey, powder is light grey.
Final wall morphology (25 layers)
Single direction (forward-forward) scan
Alternating directions (back and forth) scan
Spot melting

## Slide 16: KiSSAM as a digital twin: Optimizing part morphology with spot melting scanning strategy
B. Korneev et.al. Spot melting improves the morphology of ultrathin wall builds: a numerical study. Progress in Additive Manufacturing, 10(12), 10477-10485 (2025).

## Slide 17: Optimization of printing parameters for the “bridge” overhang structure: laser power modulation
A. Ashby et. al. Additive Manufacturing, V. 53, May 2022, 102669
Case E
Case A
Case F
MODEL

## Slide 18: Microstructure properties: simulating impact of the printing regime on grain structure for thin walls (SS316L)
The amount of long grains with <100> crystallographic orientation decreases at higher scan velocities.
Melt pool becomes longer and fragments
The amount of long 100 grains decreases
Wall longitudinal cross-sections
S. Belousov et.al. Variations in morphology and microstructure caused by different melt pool dynamics in laser powder bed fusion of ultrathin walls, in: SIM-AM2025. URL https://www.scipedia.com/public/Belousov_et_al_2026a

## Slide 19: Simulating process monitoring during PBF
A. Zakirov et. Al. KiSSAM: efficient simulation of melt pool dynamics during PBF using GPUs, Progress in Additive Manufacturing. 18 p. (2024)
Photodiode sensor response examples for EB-PBF for different scan velocities
Local temperature probes
Photodiode sensors
Back-scattered electron sensors
Photodiode sensor scheme

## Slide 20: Simulating surface quality and porosity
Electron beam size: 880 um
Velocity: 4.27 m/s
Scan: zigzag
Hatch spacing: 0.26 mm
Time delay: 6.17 ms
Electron beam size: 880 um
Velocity: 4.27 m/s
Scan: zigzag
Hatch spacing: 0.20 mm
Time delay: 9.4 ms
A. Zakirov et. Al. KiSSAM: efficient simulation of melt pool dynamics during PBF using GPUs, Progress in Additive Manufacturing. 18 p. (2024)
Increased delay between successive tracks leads to lower integral heat input and increased porosity

## Slide 21: Complex scanning strategies: a wobbling scan

## Slide 22: Multi-beam modeling
2x2 mm2 sample
4 beams
Independent beam paths
Any time gap between beams
Any number of beams

## Slide 23: Multi-beam modeling: decreasing roughness with a post-heating defocused beam
No post-heating: single beam, zig-zig strategy on powder layer
Postheating: two beams moving one after another, second beam is defocused, zig-zig strategy on powder layer.
Without post-heating, lack-of-fusion regions are observed (note the light green spots).
Post-heating improves the uniformity of melt penetration with depth (almost no spots).

## Slide 24: Selected publications
S. Belousov et.al. Variations in morphology and microstructure caused by different melt pool dynamics in laser powder bed fusion of ultrathin walls, in: SIM-AM2025. URL https://www.scipedia.com/public/Belousov_et_al_2026a.
J. Plewinski et.al., Impact of Modeling Assumptions on Simulated Melt Pool Dynamics Compared to High-Speed X-ray Observations, in: Mathematical Modeling of Weld Phonomena, vol. 14, p. 195 (2026).
B. Korneev et.al.. Spot melting improves the morphology of ultrathin wall builds: a numerical study. Progress in Additive Manufacturing, 10(12), 10477-10485 (2025).
S. Chernyshikhin et.al. Surface tension measurements of NiTi alloy for the melt pool simulation during Laser Powder Bed Fusion. Materials Letters, 139696 (2025).
A. Zakirov et.al.. KiSSAM: Efficient Simulation of Melt Pool Dynamics during PBF using GPUs. Progress in Additive Manufacturing 9 (5), 1491-1508 (2024).
M. Bogdanova et.al. Mesoscale Simulation of Laser Powder Bed Fusion with an Increased Layer Thickness for AlSi10Mg Alloy. Journal of Manufacturing and Materials Processing, 8(1), 7 (2024).
B. Korneev et.al. A numerical study of powder wetting influence on the morphology of laser powder bed fusion manufactured thin walls. Additive Manufacturing, 74, 103705 (2023).
A. Zakirov et.al. Predictive modeling of laser and electron beam powder bed fusion additive manufacturing of metals at the mesoscale. Additive Manufacturing, 35, 101236. (2020).
D. Nakapkin et al. Finding Optimal Parameter Ranges for Laser Powder Bed Fusion with Predictive Modeling at Mesoscale, Sim-AM 2019 (2019)

## Slide 25: KiSSAM licensing and collaboration options
Web-interface at https://kissam.cloud (cloud simulation capability)
Trial license (including cloud)
Commercial and academic licenses available
EOM module
Joint research projects with industrial partners

## Slide 26: Thank you for your attention!
Visit https://kissam.cloud to know more about KiSSAM and get your free trial
Join the growing community of KiSSAM users and collaborators!
and more...

## Slide 29: KiSSAM: A high-fidelity simulation at the mesoscale
Solver: Temperature Lattice Boltzmann Method (LBM) with free surface tracking
Powder coating simulation
Verified material library
microstructure
Full part simulations
Scanning strategy import directly from 3D-printers (G-code)
Beam shaping
Laser and electron beam
A. Zakirov et.al. Additive Manufacturing, 35, 101236 (2020); Progress in Additive Manufacturing, 9, 1491 (2024).
Porosity and roughness prediction

## Slide 30: Previously with KiSSAM…
Process map generation
D. Nakapkin et.al., Sim-AM 2019: II International Conference on Simulation for Additive Manufacturing (pp. 297-308). CIMNE (2019).
Study of thicker powder layers as a means to increase productivity of PBF
M. Bogdanova et.al., Journal of Manufacturing and Materials Processing, 8(1), 7 (2024).
Prediction of the thin wall morphology at the mesoscale
B. Korneev et.al., Additive Manufacturing, 74, 103705 (2023).

## Slide 31: Bulk porosity prediction
1 – Yildiz, R. A., Popa, A. A., & Malekan, M. (2024). On the effect of small laser spot size on the mechanical behaviour of 316L stainless steel fabricated by L-PBF additive manufacturing. Materials Today Communications, 38, 108168..
2x2 mm2 sample
Height map
Density map, top view
GOAL1 |  | SOLUTION |  | ANALYSIS |  | OUTCOME
Determine porosity of bulk sample with different scanning strategies |  | Multylayer modeling with rotated pattern at each layer. Utilization of the time gap between successive tracks to avoid melt pool overlap |  | Quality of remelted material, porosity and microporosity |  | Optimal strategy to decrease porosity
6 layers

## Slide 32: Basic Model Validation on cross-sections
A. Zakirov et.al. Additive Manufacturing, 35, 101236 (2020); Progress in Additive Manufacturing, 9, 1491 (2024)
A
B
C
AMMT
A
B
C
CBM
Source | Beam size, um | Velocity, m/s | Power, W | Material
Laser | 100, 170 | 0.4 – 1.2 | 137.9 - 195 | Inconel 625
B. Lane et al. Integrating Materials and Manufacturing Innovation volume 9, 16–30 (2020)
Source | Beam size, um | Velocity, m/s | Current, mA / Voltage, KV | Material
E-beam | 500 | 1, 3, 6 | 15 mA 60 kV | Ti-6Al-4V
ELECTRON BEAM PBF
LASER PBF

## Slide 33: Advanced Validation on different experimental data
Validation with cross-sections
1 m/s, 300 W
0.4 m/s, 350 W
1 m/s, 350 W
0.4 m/s, 400 W
1 m/s, 400 W
EXPERIMENT
MODELING
Validation with SEM data
MODELING
EXPERIMENT
MODELING – longitudinal cross-sections
Notes: Упростить и назвать его «валидация»

## Slide 34: Process Monitoring: Photodiode sensor response during thin wall build with EB-PBF
See our paper: A. Zakirov et. Al. KiSSAM: efficient simulation of melt pool dynamics during PBF using GPUs, Progress in Additive Manufacturing. 18 p. (2024)
Beam power 1700 W;
Scan speed 4.3 m/s;
Beam size (D4s) 900 um;
Platform step 50 um
Sensor signal gradually grows as the build progresses, indicating heat build up in the thin wall.

## Slide 35: Motivation
heat input
melting & hydrodynamics & solidification & thermals
morphology: roughness & porosity
microstructure, mechanical properties etc.
Process
Quality
Quality
Process
dictates
defines
Experiment?
Some things are hard to measure
Process parameters adjustment is time-consuming…
High costs…
Why don’t we go for…
simulation?